SECTION 09 29 00

GYPSUM BOARD

THIS SECTION IS WRITTEN IN CSI 3-PART FORMAT AND IN CSI PAGE FORMAT; THE PROJECT NAME/NUMBER/DATE AND SECTION TITLE IN THE FOOTER ARE OPTIONAL. NOTES TO THE SPECIFIER, SUCH AS THIS, MUST BE DELETED FROM THE FINAL SPECIFICATION.

IT IS ASSUMED THAT THE GENERAL CONDITIONS BEING USED ARE AIA A201-1997.

PART	1	GENERAL

1.01	SUMMARY

A.	Section Includes: Glass-mat faced, moisture resistant gypsum board.

EDIT LIST BELOW TO CONFORM TO PROJECT REQUIREMENTS. VERIFY SECTION NUMBERS AND TITLES.

B.	Related Sections:

1.	Section 06 10 00 Rough Carpentry.

2.	Section 09 21 16 Gypsum Board Assemblies.

3.	Section 09 22 00 Supports for Plaster and Gypsum Board.

IF THE PROJECT INCLUDES ALLOWANCES OR ALTERNATES OR UNIT PRICES, RETAIN PARAGRAPHS BELOW AND COORDINATE WITH DIVISION 01.

C.	Allowances:

D.	Unit Prices:

E.	Alternates:

1.02	REFERENCES

A.	ASTM International (ASTM):

1.	ASTM C473 Standard Test Methods for Physical Testing of Gypsum Panel Products.

2.	ASTM C518 Standard Test Method for Steady-State Thermal Transmission Properties by Means of the Heat Flow Meter Apparatus.

3.	ASTM C630 Standard Specification for Water-Resistant Gypsum Backing Board.

4.	ASTM C840 Standard Specification for Application and Finishing of Gypsum Board.

5.	ASTM C1396 Standard Specification for Gypsum Board.

6.	ASTM C1658 Standard Specification for Glass Mat Gypsum Panels.

7.	ASTM D3273 Standard Test Method for Resistance to Growth of Mold on the Surface of Interior Coatings in an Environmental Chamber.

8.	ASTM E84 Standard Test Method for Surface Burning Characteristics of Building Materials.

B.	Gypsum Association (GA): GA-214 Recommended Levels of Gypsum Board Finish.

1.03	SUBMITTALS

A.	Product Data: Manufacturer’s specifications and installation instructions for each product specified.

1.04	QUALITY ASSURANCE

RETAIN BELOW IF REQUIRED, REVISE LIMITS IF REQUIRED.

A.	Regulatory Requirements: Provide products that comply with the following limits for surface burning characteristics when tested per ASTM E84:

1.	Flame spread: 25, maximum.

2.	Smoke developed: 450, maximum.

B.	Provide products that have been GREENGUARD Indoor Air Quality Certified by the GREENGUARD Environmental Institute under the GREENGUARD Standard for Low Emitting Products and GREENGUARD for Children & Schools product certification program.

COORDINATE ARTICLE BELOW WITH PROJECT REQUIREMENTS.

1.05	WARRANTY

A.	Provide products that offer six months of coverage against in-place exposure damage (delamination, deterioration and decay).

B.	Manufacturer’s Warranty: Three years against manufacturing defects.

THIS GUIDE SPEC WAS WRITTEN TO PROVIDE THREE EDITING OPTIONS: 1) PROPRIETARY, 2) GENERIC, OR 3) A COMBINATION OF THE TWO.

PART	2	PRODUCTS

IF PROPRIETARY PRODUCT NAMES ARE INCLUDED IN THE “MATERIALS” ARTICLE BELOW, DELETE THIS ARTICLE ALTOGETHER. IF A PROPRIETARY SPECIFICATION IS REQUIRED, RETAIN THIS ARTICLE AND DELETE THE “MATERIALS” ARTICLE.

2.01	MANUFACTURERS

EDIT LISTS BELOW TO CONFORM TO PROJECT REQUIREMENTS. IF OTHER MANUFACTURERS ARE BEING ADDED TO THIS SECTION, ADD LISTINGS OF THEIR PROPRIETARY PRODUCT NAMES.

A.	Georgia-Pacific Gypsum LLC:

1.	Fiberglass-Mat Faced Gypsum Board: DensArmor Plus.

2.	Fire-Rated Fiberglass-Mat Faced Gypsum Board: DensArmor Plus Fireguard.

B.

C.

THIS ARTICLE INCLUDES GENERIC DESCRIPTIONS OF GYPSUM BOARD PANELS; THE NAMES OF THE CORRESPONDING GEORGIA-PACIFIC GYPSUM PRODUCTS ARE INCLUDED AS ACCEPTABLE PRODUCTS. IF THIS SECTION IS BEING EDITED TO BE GENERIC, THESE PRODUCT NAMES SHOULD BE DELETED.

IF OTHER MANUFACTURERS ARE BEING ADDED TO THIS SECTION, 1) ADD THE PROPRIETARY PRODUCT NAMES OF THOSE MANUFACTURERS, OR 2) IF PROPRIETARY NAMES ARE LISTED IN THE “MANUFACTURERS” ARTICLE ABOVE, DELETE THEM FROM THIS ARTICLE ALTOGETHER.

2.02	MATERIALS

A.	Fiberglass-Mat Faced Gypsum Board:

1.	Thickness: 1/2 inch.

2.	Width: 4 feet.

3.	Length: 8 feet.

4.	Weight: 2020 pounds per M square feet.

5.	Edges: Tapered.

6.	Surfacing: Coated fiberglass mat on face, back, and long edges.

7.	Flexural Strength, Parallel (ASTM C473, ASTM C1658): Not less than 80 lbf.

8.	Flexural Strength, Perpendicular (ASTM C473, ASTM C1658): Not less than 100 lbf.

9.	R-Value (ASTM C518): Not less than 0.56.

10.	Nail Pull Resistance (ASTM C473, ASTM C1658): Not less than 80 lbf.

11.	Humidified Deflection (ASTM C473, ASTM C1658): Not more than 1/4 inch.

12.	Hardness, Core, Edges, and Ends (ASTM C473, ASTM C1396): Not less than 15.

13.	Water Absorption (ASTM C630, ASTM C1396, ASTM C1658): Less than 5 percent of weight.

14.	Mold Resistance (ASTM D3273): 10, in a test as manufactured.

15.	Acceptable Products:

a.	1/2 inch DensArmor Plus Interior Guard, Georgia-Pacific Gypsum.

b.	1/2 inch DensArmor Plus Fireguard Interior Guard Type C, Georgia-Pacific Gypsum.

c.

B.	5/8 Inch Fire-Rated Fiberglass-Mat Faced Gypsum Board:

1.	Thickness: 5/8 inch.

2.	Width: 4 feet.

3.	Length: 8 feet.

4.	Weight: 2570 pounds per M square feet.

5.	Edges: Tapered.

6.	Surfacing: Coated fiberglass mat on face, back, and long edges.

7.	Flexural Strength, Parallel (ASTM C473, ASTM C1658): Not less than 100 lbf.

8.	Flexural Strength, Perpendicular (ASTM C473, ASTM C1658): Not less than 140 lbf.

9.	R-Value (ASTM C518): Not less than 0.67.

10.	Nail Pull Resistance (ASTM C473, ASTM C1658): Not less than 90 lbf.

11.	Humidified Deflection (ASTM C473, ASTM C1658): Not more than 1/8 inch.

12.	Hardness, Core, Edges, and Ends (ASTM C473, ASTM C1396): Not less than 15.

13.	Water Absorption (ASTM C630, ASTM C1396, ASTM C1658): Less than 5 percent of weight.

14.	Mold Resistance (ASTM D3273): 10, in a test as manufactured.

15.	Acceptable Products:

a.	5/8 Inch DensArmor Plus Fireguard Interior Guard Type X, Georgia-Pacific Gypsum.

b.	5/8 Inch DensArmor Plus Abuse Guard, Georgia-Pacific 						Gypsum.

c.

C.	1/2 Inch Fire-Rated Fiberglass-Mat Faced Gypsum Board:

1.	Thickness: 1/2 inch.

2.	Width: 4 feet.

3.	Length: 8 feet.

4.	Weight: 2020 pounds per M square feet.

5.	Edges: Tapered.

6.	Surfacing: Coated fiberglass mat on face, back, and long edges.

7.	Flexural Strength, Parallel (ASTM C473, ASTM C1658): Not less than 80 lbf.

8.	Flexural Strength, Perpendicular (ASTM C473, UL File No. R2717): Not less than 120 lbf.

9.	R-Value (ASTM C518): Not less than 0.56.

10.	Nail Pull Resistance (ASTM C473, ASTM C1658): Not less than 80 lbf.

11.	Humidified Deflection (ASTM C473, ASTM C1658): Not more than 1/4 inch.

12.	Hardness, Core, Edges, and Ends (ASTM C473, ASTM C1396): Not less than 15.

13.	Water Absorption (ASTM C630, ASTM C1396, ASTM C1658): Less than 5 percent of weight.

14.	Mold Resistance (ASTM D3273): 10, in a test as manufactured.

15.	Acceptable Products:

a.	1/2 Inch DensArmor Plus Fireguard Interior Guard Type C, Georgia-Pacific Gypsum.

b.

c.

PART	3	EXECUTION

3.01	INSTALLATION

A.	General: In accordance with ASTM C840 and the manufacturer’s recommendations.

IF OTHER MANUFACTURERS WERE ADDED IN PART 2, REFERENCE THEIR INSTALLATION RECOMMENDATIONS BELOW BY TITLE.

1.	Manufacturer’s Recommendations:

a.	Current “Product Catalog”, Georgia-Pacific Gypsum.

b.

c.

3.02	APPLICATION

RETAIN PARAGRAPH BELOW WHEN “LEVEL 4” FINISH IS REQUIRED PER GA-214. WHEN USING GLOSS, SEMI-GLOSS OR ENAMEL PAINT, OR WHEN WORKING IN A CRITICAL (SEVERE) LIGHTING AREA, ALWAYS FINISH TO A “LEVEL 5” FINISH PER GA-214. REFER TO GA-214 FOR DEFINITION AND EXAMPLES OF CRITICAL LIGHT AREAS. CONSULT GYPSUM BOARD MANUFACTURER FOR MORE INFORMATION.

A.	Primer and Paint Application:

1.	Use a high quality, high build drywall primer/surfacer. Comply with application instructions of the primer manufacturer as stated on the container.

2.	Apply high build primer at a sufficient wet film thickness to ensure a dry film thickness that will produce acceptable results.

THE NUMBER OF COATS OF FINISH PAINT AND THE TOTAL DRY FILM THICKNESS OF THE FINISH COATS NEEDED FOR ACCEPTABLE RESULTS WILL DEPEND ON THE PAINT USED. CONSULT PAINT MANUFACTURER FOR MORE INFORMATION.

3.	Apply finish coats of paint per the paint manufacturer’s label instructions.

3.03	PROTECTION

REVISE BELOW IF OTHER THAN AIA GENERAL CONDITIONS ARE USED.

A.	Protect gypsum board installations from damage and deterioration until the date of Substantial Completion.

END OF SECTION 09 29 00