GYPSUM CEMENT UNDERLAYMENT

RECOMMENDED SPECIFICATION FOR GYP-CRETE( FLOOR UNDERLAYMENT IN 
MULTIFAMILY HOUSING (LEVEL-RIGHT( CEMENTITIOUS UNDERLAYMENT IN HARD SURFACE AREAS)

PART 1	GENERAL

1.01		SUMMARY

- This is the recommended specification for Gyp-Crete Floor Underlayment in multifamily housing (Level-Right in hard surface areas).

1.02			SECTION INCLUDES

- Gyp-Crete gypsum cement

- Level-Right cementitious underlayment

- Maxxon Floor Primer

- Maxxon Overspray

- Reinforcement mesh

1.03			QUALITY ASSURANCE

- Installer's Qualifications:  Installation of Gyp-Crete and Level-Right shall be by an applicator authorized by the Maxxon Corporation using Maxxon approved mixing and pumping equipment.

1.04		DELIVERY, STORAGE AND HANDLING

- General Requirements:  Materials shall be delivered in their original, unopened packages, and protected from exposure to the elements.  Damaged or deteriorated materials shall be removed from the premises.

1.05		SITE CONDITIONS

- Environmental Requirements:  Before, during and after installation of Gyp-Crete and 
Level-Right, building interior shall be enclosed and maintained at a temperature above 50 degrees F (10 degrees C) and below 100 degrees F (37.7 degrees C) until structure and subfloor temperatures are stabilized.

PART 2	PRODUCTS

2.01		MATERIALS

- Gypsum Cement:  Floor underlayment Gyp-Crete as manufactured by the Maxxon Corporation, Hamel, MN.  All others must receive prior approval.

- Cementitious Underlayment:  Level-Right cementitious underlayment as manufactured by the Maxxon Corporation, Hamel, MN.  All others must receive prior approval.

- Sand Aggregate:  Sand shall be 1/8 inch (3 mm) or less, washed masonry or plaster sand, meeting requirements of Maxxon Corporation Sand Specifications 101.

- Mix Water:  Potable, free from impurities.

- Subfloor Primer:  Maxxon Floor Primer

- Sealer:  Maxxon Overspray

- Reinforcement mesh:  Diamond metal lath or Maxxon plastic galvanized net must be used over wood subfloors in all areas to receive Level-Right.  The reinforcement mesh is not necessary over concrete or precast subfloors.

2.02		MIX DESIGNS

- General Requirements:  Mix proportions and methods shall be in strict accordance with product manufacturer recommendations.

PART 3	EXECUTION

3.01	PREPARATION

- Condition and Cleaning of Subfloor:  Subfloor shall be structurally sound.  General Contractor shall clean subfloor to remove mud, oil, grease, and other contaminating factors before the arrival of the underlayment crew.

- Leak Prevention:  Fill cracks and voids with a quick setting patching or caulking material where leakage of underlayment could occur.

- Priming Subfloor:  Prime the subfloor using the Maxxon Floor Primer per manufacturer’s recommendations.  Priming instructions may vary according to the porosity of the substrate, multiple coats may be necessary over porous plank or concrete.

- Reinforcement mesh:  Staple the diamond metal lath or Maxxon plastic net to the wood subfloor, overlapping the lath or net where it meets.  This is done in the Level-Right underlayment areas only.

3.02	APPLICATION OF CEMENTITIOUS FLOORING

- Scheduling:  Application of Gyp-Crete and Level-Right shall not begin until the building is enclosed, including roof, windows, doors, and other fenestration.  Schedule application of 
Gyp-Crete after installation of gypsum board work.

- Application:  Place Gyp-Crete and Level-Right at 3/4 inch (19 mm) minimum over wood frame, 1/2 inch (13 mm) minimum over plank or poured in place concrete.  Spread and screed underlayments to a smooth surface.  Except at authorized joints, place Gyp-Crete as continuously as possible until application is complete so that no Gyp-Crete product slurry is placed against Gyp-Crete product that has obtained its initial set.

- Drying:  General Contractor shall provide continuous ventilation and adequate heat to rapidly remove moisture from the area until the underlayment products are dry.  General Contractor shall provide mechanical ventilation if necessary.  Under the above conditions, for 3/4 inch (19 mm) thick Gyp-Crete, 5-7 days is usually adequate drying time.  To test for dryness, tape a 24 inch by 24 inch (609 mm by 609 mm) section of plastic or high density rubber mat to the surface of the underlayment.  After 48-72 hours, if no condensation occurs, the underlayment shall be considered dry.  Perform dryness test 5-7 days after pour.

3.03	PREPARATION FOR INSTALLATION OF GLUE DOWN FLOOR GOODS

- Sealing:  Seal all areas that receive glue down floor goods with Maxxon Overspray according to the Maxxon Corporation's specifications.  Any floor areas where the surface has been damaged shall be cleaned and sealed regardless of floor covering to be used.  Where floor goods manufacturers require special adhesive or installation systems, their requirements supersede these recommendations.

- Floor Goods Procedures:  See the Maxxon Corporation's "Procedures for Attaching Finished Floor Goods to Maxxon Underlayments" brochure for guidelines for installing finished floor goods.  This procedure is not a warranty and is to be used as a guideline only.

3.04	FIELD QUALITY CONTROL

- Slump Test:  Gyp-Crete and Level-Right mix shall be tested for slump as it is being pumped using a 2 inch by 4 inch (50 mm by 101 mm) cylinder resulting in a patty size of 8 inches (203 mm) plus or minus 1 inch (25 mm) diameter.

- Field Samples:  At least one set of 3 molded cube samples shall be taken from each day's pour during the Gyp-Crete and Level-Right product application.  Gyp-Crete must be tested as recommended by the Maxxon Corporation in accordance with modified ASTM C 472.  
Level-Right must be tested as recommended by the Maxxon Corporation in accordance with modified ASTM C109.  Test results shall be available to architect and/or contractor upon request from applicator.

3.05	PROTECTION

- Protection From Heavy Loads:  During construction, place temporary wood planking over 
Gyp-Crete and Level-Right products wherever they will be subject to heavy wheeled or concentrated loads.

END OF SECTION