SELF-LEVELING CONCRETE FLOOR UNDERLAYMENT

RECOMMENDED SPECIFICATION FOR LEVEL-RIGHT( FS-10 CEMENTITIOUS 
SELF-LEVELING FLOOR UNDERLAYMENT OVER PRECAST CONCRETE SLABS

PART 1	GENERAL

1.01		SUMMARY

- This is the recommended specification for Level-Right FS-10 Cementitious Self-Leveling Floor Underlayment over precast concrete slabs.

1.02			SECTION INCLUDES

- Level-Right FS-10 Cementitious Self-Leveling Floor Underlayment

- Manufacturer Approved Primer

1.03			QUALITY ASSURANCE

- Installer's Qualifications:  Installation of Level-Right FS-10 shall be by an applicator authorized by the Maxxon Corporation using Maxxon approved mixing and pumping equipment.

1.04		DELIVERY, STORAGE AND HANDLING

- General Requirements:  Materials shall be delivered in their original, unopened packages, and protected from exposure to the elements.  Damaged or deteriorated materials shall be removed from the premises.

1.05		SITE CONDITIONS

- Environmental Requirements:  Before, during and after installation of Level-Right FS-10, building interior shall be enclosed and maintained at a temperature above 50 degrees F (10 degrees C) and below 100 degrees F (37.7 degrees C) until structure and subfloor temperature are stabilized.

PART 2	PRODUCTS

2.01		MATERIALS

- Cementitious Self-Leveling Poured Floor Underlayment:  Floor underlayment compound shall be Level-Right FS-10 Cementitious Self-Leveling Floor Underlayment as manufactured by Maxxon Corporation, Hamel, MN.

- Mix Water:  Potable, free from impurities.

- Precast Primer:  Manufacturer Approved Primer

2.02		MIX DESIGNS

- General Requirements:  Level-Right FS-10 mix proportions and methods shall be in strict accordance with product manufacturer recommendations.

PART 3	EXECUTION

3.01	PREPARATION

- Condition and Cleaning of Precast:  Precast shall be structurally sound. General Contractor shall clean precast to remove mud, oil, grease, and other contaminating factors before arrival of the Level-Right FS-10 underlayment crew.

- Leak Prevention:  Fill cracks and voids with a quick setting patching or caulking material where leakage of Level-Right FS-10 could occur.

- Priming Precast:  Prime precast using the Manufacturer Approved Primer.  Priming instructions vary according to the porosity of the precast, multiple coats may be necessary.

- Expansion Joints:  Allow joints to continue through the Level-Right FS-10 at the same width.

3.02	APPLICATION OF SELF-LEVELING FLOORING

- Scheduling:  Application of Level-Right FS-10 shall not begin until the building is enclosed, including roof, windows, doors, and other fenestration.  Install after drywall installation unless tenant finish requirements identify partitioning after the pour.

- Application:  Place Level-Right FS-10 0 - 1/2” (0 - 13 mm). Deeper applications can be done in multiple lifts. Spread and float Level-Right FS-10 to a smooth surface.  Except at authorized joints, place Level-Right FS-10 as continuously as possible until application is complete so that no Level-Right FS-10 slurry is placed against Level-Right FS-10 product that has obtained its initial set.

- Drying:  General Contractor shall provide continuous ventilation and adequate heat until 
Level-Right FS-10 is dry.  General contractor shall provide mechanical ventilation if necessary.

3.03	PREPARATION FOR INSTALLATION OF GLUE DOWN FLOOR GOODS

- Floor Goods Attachment:  See the brochure "Procedures for Attaching Finished Floor Goods to Maxxon Underlayments" for guidelines for installing finished floor goods.  This procedure is not a warranty and is to be used as a guideline only.

3.04	FIELD QUALITY CONTROL

- Field Samples:  At least one set of 3 molded cube samples shall be taken from each day's pour during the Level-Right FS-10 application.  Cubes shall be tested as recommended by the
Maxxon Corporation in accordance with modified ASTM C 109.  Test results shall be available to architect and/or contractor upon request from applicator.

3.05     PROTECTION

- Protection From Heavy Loads:  During construction, place temporary wood planking over 
Level-Right FS-10 wherever it will be subject to heavy wheeled or concentrated loads.

END OF SECTION