SELF-LEVELING CEMENTITIOUS TOPPING

RECOMMENDED SPECIFICATION FOR LEVEL-RIGHT( WEARTOP OVER

ACOUSTI-MAT( LP SOUND DEADENING PAD OVER CONCRETE

PART 1	GENERAL

1.01		SUMMARY

- This is the recommended specification for Level-Right WearTop over Acousti-Mat LP sound deadening pad over concrete.

1.02			SECTION INCLUDES

- Level-Right WearTop

- Acousti-Mat LP

- Acousti-Mat LP Adhesive

- Maxxon WearTop Curing Agent

- Pioneer Eclipse Hard Floor Sealer & Envirostar Green Satin Top Coat

1.03			QUALITY ASSURANCE

- Level-Right WearTop Installer's Qualifications:  Installation of Level-Right WearTop shall be by an applicator authorized by the Maxxon Corporation using Maxxon approved mixing and pumping equipment.

- Acousti-Mat LP Installer's Qualifications:  Installation of Acousti-Mat LP shall be by an applicator authorized by the Maxxon Corporation.

1.04		DELIVERY, STORAGE AND HANDLING

- General Requirements:  Materials shall be delivered in their original, unopened packages, and protected from exposure to the elements.  Damaged or deteriorated materials shall be removed from the premises.

1.05		SITE CONDITIONS

- Environmental Requirements:  Before, during and after installation of Level-Right WearTop and Acousti-Mat LP, building interior shall be enclosed and maintained at a temperature above 50 degrees F (10 degrees C).

PART 2	PRODUCTS

2.01		MATERIALS

- Underlayment: Recommended Level-Right WearTop as manufactured by the Maxxon Corporation, Hamel, MN.

- Sound Deadening Pad:  Acousti-Mat LP as manufactured by the Maxxon Corporation, Hamel, MN.

- Sand Aggregate:  Sand shall be 1/8 inch (3 mm) or less, washed masonry or plaster sand, meeting requirements of Maxxon Corporation Sand Specifications 101.

- Mix Water:  Potable, free from impurities

- Adhesive:  Acousti-Mat LP Adhesive as manufactured by the Maxxon Corporation, Hamel, MN.

- Sealer:  Maxxon WearTop Curing Agent

- Wax:  Pioneer Eclipse Hard Floor Sealer and Envirostar Green Satin Top Coat

2.02		MIX DESIGNS

- General Requirements:  Mix proportions and methods shall be in strict accordance with product manufacturer recommendations.

PART 3	EXECUTION

3.01	PREPARATION

- Condition and Cleaning of Subfloor:  Subfloor shall be structurally sound.  General Contractor shall clean subfloor to remove mud, oil, grease, and other contaminating factors before the arrival of the Level-Right WearTop and Acousti-Mat LP crew.

- Leak Prevention:  Fill cracks and voids with a quick setting patching or caulking material where leakage of adhesive could occur.

- Expansion Joints:  Allow joints to continue through the Level-Right WearTop at the same width.

3.02	APPLICATION OF ACOUSTI-MAT LP AND REINFORCEMENT MESH

- Acousti-Mat LP Installation:  Install Acousti-Mat LP following manufacturer’s recommendations and specifications.

3.03	APPLICATION OF SELF-LEVELING FLOORING

- Scheduling:  Application of Level-Right WearTop and Acousti-Mat LP shall not begin until the building is enclosed, including roof, windows, doors, and other fenestration.  Install after drywall installation unless tenant finish requirements identify partitioning after the pour.

- Application:  Place the recommended   Level-Right WearTop a nominal 3/8 inch (8mm) thick over Acousti-Mat LP.  Spread and screed Level-Right WearTop to a smooth surface

- Sanding for Burnished, Marble Look:  Buff sand the WearTop surface the day after the pour with a traditional floor buffing machine using an 80, 100 or 120 mesh screen to desired look. After the surface is screen sanded and broomed, use a tack rag or dry Swiffer mop to remove dust.

- Curing and Sealing:  Level-Right WearTop is to be coated with at least 2 coats of Maxxon approved sealer such as Maxxon WearTop Curing Agent within 24 hours after installation except when an epoxy or other floor coverings will be installed.

- Wax:  Apply wax after the WearTop Curing Agent is dry using 2 coats of Pioneer Eclipse Hard Floor Sealer followed by 2 coats of Envirostar Green Satin Top Coat.  Follow manufacturer’s instructions on the label.

- Drying:  General Contractor shall provide continuous ventilation and adequate heat until 
Level-Right WearTop is fully cured.

3.04	PREPARATION FOR INSTALLATION OF GLUE DOWN FLOOR GOODS

- Floor Goods Procedures:  See the Maxxon Corporation's "Procedures for Attaching Finished Floor Goods to Maxxon Underlayments" brochure for guidelines for installing finished floor goods.  This procedure is not a warranty and is to be used as a guideline only.

3.05	FIELD QUALITY CONTROL

- Slump Test:   Level-Right WearTop mix shall be tested for slump as it's being pumped using a 2 inch by 4 inch (50 mm by 101 mm) cylinder resulting in a patty size of 9 1/2 inches (241 mm) plus or minus 1 inch (25 mm) diameter.

- Field Samples:  At least one set of 3 molded cube samples shall be taken from each day's pour during the Level-Right WearTop application.  Cubes shall be tested as recommended by the Maxxon Corporation in accordance with modified ASTM C 109.  Test results shall be available to architect and/or contractor upon request from applicator.

3.06	PROTECTION

- Protection From Heavy Loads:  During construction, place temporary wood planking over 
 Level-Right WearTop wherever it will be subject to heavy wheeled or concentrated loads.

END OF SECTION