RECOMMENDED SPECIFICATION FOR LEVEL-RIGHT( WEARTOP™ CEMENTITIOUS 
SELF-LEVELING FLOOR TOPPING OVER MAXXON® GYPSUM FLOOR UNDERLAYMENTS, WITH OPTIONAL ACOUSTI-MAT® SOUND MATS OR WITH OPTIONAL RADIANT HEAT SYSTEMS

PART 1	GENERAL

1.01		SUMMARY

A.	This is the recommended specification for Level-Right WearTop Cementitious Self-Leveling Floor Topping over Maxxon Gypsum Floor Underlayments, with optional Acousti-Mat Sound Mats or with optional Radiant Heat Systems.

1.02			SECTION INCLUDES

A.	Level-Right WearTop Cementitious Self-Leveling Floor Topping

B.	Maxxon Gypsum Underlayment

C.  WearTop Bonder

D.	Maxxon Acrylic Sealer

E.  	WearTop Curing Agent

F.	Optional – Maxxon Sound Mats – Acousti-Mat II, Enkasonic or Acousti-Mat 3.

G.  Electric or hydronic radiant floor heat.

1.03			QUALITY ASSURANCE

A.	Level-Right WearTop and Maxxon Gypsum Underlayment

Installer's Qualifications:  Installation of Level-Right WearTop and Maxxon Gypsum Underlayment shall be by an applicator authorized by the Maxxon Corporation using Maxxon approved mixing and pumping equipment.

B.	Sound Mats – Acousti-Mat II, Enkasonic or Acousti-Mat 3: Installation of Acousti-Mat II, Enkasonic or Acousti-Mat 3 shall be by an applicator authorized by Maxxon Corporation.

1.04		DELIVERY, STORAGE AND HANDLING

A.	General Requirements:  Materials shall be delivered in their original, unopened packages, and protected from exposure to the elements.  Damaged or deteriorated materials shall be removed from the premises.

1.05		SITE CONDITIONS

- Environmental Requirements:  Before, during and after installation of all Maxxon products, building interior shall be enclosed and maintained at a temperature above 50 degrees F (10 degrees C) and below 100 degrees F (37.7 degrees C) until structure and subfloor temperature are stabilized.

PART 2	PRODUCTS

2.01		MATERIALS

- Level-Right WearTop:  Level-Right WearTop Cementitious Self-Leveling Floor Topping as manufactured by Maxxon Corporation, Hamel, MN.

- Maxxon Gypsum Underlayment:  Recommended Maxxon Gypsum Underlayment as manufactured by Maxxon Corporation, Hamel, MN.

- Maxxon Acrylic Sealer:  Maxxon Acrylic Sealermanufactured by Maxxon Corporation, Hamel, MN.

- WearTop Bonder:  WearTop Bonder manufactured by Maxxon Corporation, Hamel, MN.

- WearTop Curing Agent:  Maxxon Curing Agent as manufactured by Maxxon Corporation, Hamel, MN

- Optional Sound Mats:  Acousti-Mat II, Enkasonic or Acousti-Mat 3 manufactured by Maxxon Corporation, Hamel, MN.

2.02		MIX DESIGNS

- General Requirements:  Mix proportions and methods shall be in strict accordance with Maxxon Corporation, Hamel, MN.

PART 3	EXECUTION

3.01	PREPARATION

A.	Condition and Cleaning of Subfloor:  Subfloor shall be structurally sound.  General Contractor shall clean subfloor to remove mud, oil, grease, and other contaminating factors before the arrival of the Maxxon underlayment crew.

B.	Leak Prevention:  Fill cracks and voids with a quick setting patching or caulking material where leakage of the Maxxon underlayment could occur.

C.	Priming Subfloor:  Prime the subfloor or acoustical mats using the Maxxon Floor Primer.  Priming instructions may vary according to the type of substrate, multiple coats may be necessary.

D.	Expansion Joints:  Allow joints to continue through the Maxxon Underlayment at the same width.

3.02	OPTIONAL – APPLICATION OF SOUND MATS: ACOUSTI-MAT II, ENKASONIC OR ACOUSTI-MAT 3

A.	Install Acousti-Mat II, Enkasonic or Acousti-Mat 3 in strict accordance with Maxxon Corporation specifications and recommendations.

3.03      APPLICATION OF MAXXON GYPSUM UNDERLAYMENT AND LEVEL-RIGHT

WEARTOP

A.  Scheduling:  Application of Maxxon Gypsum Underlayment and Level-Right WearTop shall       not begin until the building is enclosed, including roof, windows, doors, and other fenestration.

- Application:  Place the Maxxon Gypsum Underlayment in strict accordance with Maxxon Corporation specifications and recommendations over wood or concrete subfloors, Maxxon Sound Mats, or hot water or electric radiant heat systems.

- Dryness Test:  Maxxon Gypsum Underlayment must be tested for dryness prior to the
Level-Right WearTop application.  Use either a Delmhorst G-79 or B D 2100 moisture meter for gypsum concrete.  The moisture reading must be 5% or less.  Also a relative humidity meter or probe can be used.

- Maxxon Acrylic – WearTop Bonder – Level-Right WearTop Self Leveling Application:

Day 1:  Maxxon underlayment is sealed with 2 coats of Maxxon Acrylic at 300 sq. ft. per gallon

(dilute 4 parts water to 1 part Acrylic), approximately 1 hour between coats.

Day 2:  The WearTop Bonder is ready to use directly from the pail.  WearTop Bonder is a 2 coat application.  Allow 1-2 hours between coats.

First Coat:  Roll on with ¼” or 3/8” nap roller at a rate of 300sq. ft per gallon (1.48 m2/liter).  Allow 1-2 hours before applying 2nd coat.

Second Coat:  Roll at a rate of 300 sq. ft. per gallon (1.48 m²/liter).

Day 3:  Install Level-Right WearTop at a minimum of ¼” per manufacturer’s recommendations.

- Application of the sealer over Level-Right WearTop:  Apply a Maxxon Corporation recommended sealer or tested compatible sealer over the Level-Right WearTop within 24 hours of the pour. For additional information refer to the Maxxon WearTop Sealer Guide.

3.04	FIELD QUALITY CONTROL

A.	Slump Test:  Maxxon Gypsum Underlayment mix shall be tested for slump as its being pumped using a 2” x 4” (50 mm by 101 mm) cylinder resulting in a patty size of 8 inches (203 mm) plus or minus 1 inch (25 mm) diameter.

- Field Samples:  At least one set of 3 molded cube samples shall be taken from each day's pour during the Maxxon Gypsum Underlayment application.  Cubes shall be tested as recommended by the Maxxon Corporation in accordance with modified ASTM C 472.  At least one set of  3 molded cube samples shall be taken from each day's pour during the Level-Right WearTop application.  Cubes shall be tested as recommended by the Maxxon Corporation in accordance with modified ASTM C 109.  Test results shall be available to architect and/or contractor upon request from applicator.

  - PROTECTION

- Protection From Heavy Loads:  During construction, place temporary wood planking over the Maxxon Gypsum Underlayment and Level-Right WearTop wherever it will be subject to heavy wheeled or concentrated loads.

END OF SECTION